# SECTION 13 45 13
BALLISTIC-RESISTANT COMPOSITE WALL PANELS
LytArmor® Bravo I

# PART 1 – GENERAL

## 1.01 SUMMARY

Provide factory-manufactured concealed ballistic-resistant composite wall panels for installation within framed wall assemblies where indicated. Work includes panels, accessories, coordination with adjacent trades, and installation recommendations.

## 1.02 RELATED SECTIONS

05 40 00 Cold-Formed Metal Framing; 06 10 00 Rough Carpentry; 08 88 56 Ballistic Resistant Glazing; 09 21 16 Gypsum Board Assemblies.

## 1.03 REFERENCES

UL 752, NIJ 0101.07, NIJ 0108.01 and applicable ASTM standards.

## 1.04 PERFORMANCE REQUIREMENTS

Panels shall be manufactured from UHMWPE composite and provide UL 752 Level 1,2,3, & 6 protection together with NIJ HG2 / III-A performance where indicated. Provide multi-hit capable panels matching tested construction.

## 1.05 SUBMITTALS

Product data, shop drawings, panel layout, installation instructions, warranty, and independent ballistic test reports.

## 1.06 QUALITY ASSURANCE

Manufacturer shall specialize in ballistic protection systems and maintain documented third-party testing. Products shall be supplied by a single manufacturer.

## 1.07 DELIVERY, STORAGE AND HANDLING

Store panels flat in a dry protected environment. Prevent UV exposure, impact damage and excessive moisture prior to installation.

## 1.08 WARRANTY

Provide manufacturer's standard limited warranty.

# PART 2 – PRODUCTS

## 2.01 MANUFACTURER

Action Bullet Resistant, Inc., 235 Union Blvd, West Islip, New York.

800-962-8088 | info@actionbullet.com

## 2.02 BASIS OF DESIGN

LytArmor® Bravo I Ballistic Panel, Product Code PAVBI88M.

## 2.03 MATERIALS

Ultra High Molecular Weight Polyethylene (UHMWPE) unidirectional composite with protective PE coating.

## 2.04 PERFORMANCE

Nominal thickness 5.2 mm (0.20 in), areal density approximately 0.95 lb/ft², rigid construction, excellent UV resistance, humidity absorption less than 0.9 percent, excellent multi-hit capability.

## 2.05 BALLISTIC PERFORMANCE

Designed to meet UL 752 Level 1,2,3, & 6 and applicable NIJ handgun standards. Average backface deformation and V50 performance shall be consistent with manufacturer's published test data.

## 2.06 FABRICATION

Factory fabricate panels to project dimensions where practical. Clearly identify each panel with orientation and installation location. Custom sizes available upon request.

## 2.07 STANDARD SIZES

Supply stock or custom panel sizes to suit project requirements.

# PART 3 – EXECUTION

## 3.01 EXAMINATION

Verify framing, substrates and openings are complete and suitable before installation.

## 3.02 INSTALLATION

Install panels in accordance with Action Bullet Resistant written instructions. Maintain continuous ballistic protection around joints, corners, penetrations and transitions. Coordinate with gypsum board, framing and glazing trades.

## 3.03 FIELD MODIFICATIONS

Field cutting shall only be performed using manufacturer-approved methods. Maintain minimum edge distances and preserve ballistic integrity.

## 3.04 FIELD QUALITY CONTROL

Inspect completed installation for damage, alignment and continuity. Replace damaged panels before concealment.

## 3.05 CLEANING AND PROTECTION

Protect installed panels from construction damage until substantial completion.

# SPECIFIER NOTES

This document is intended as the basis for a CSI MasterFormat specification. Final project-specific requirements including threat level, substrate, attachment method, fire-resistance coordination, and project-specific accessories should be edited by the design professional before issuance.