SECTION 10-2641

BULLET-RESISTANT FIBERGLASS SHEET

# PART 1 	 	GENERAL

1.1 	SUMMARY

- Section Includes:

1. 	Bullet-resistant fiberglass sheet for use in [partition] [casework] [____] assemblies.

- Related Sections:

    - Division 01: Administrative, procedural, and temporary work requirements.

    - Section [06 1100 - Framing and Sheathing] [__ ____ - _______] - Wood framing to receive bullet-resistant sheet.

    - Section [06 4100 - Architectural Wood Casework] [__ ____ - _______] - Casework to receive bullet-resistant sheet.

    - Section [09 2200 - Metal Support Assemblies] [__ ____ - _______] - Metal framing to receive bullet-resistant sheet.

1.2 	REFERENCES

- ASTM International (ASTM) E119 - Standard Test Methods for Fire Tests of Building Construction and Materials.

- Underwriters Laboratories (UL) 752 - Bullet Resisting Equipment.

1.3 	SYSTEM DESCRIPTION

A. 	Design Requirements: Provide bullet-resistant sheet of “non-ricochet type" intended to permit capture and retention of attacking projectile, lessening potential of random injury or lateral penetration.

1.4 	SUBMITTALS

- Submittals for Review:

1. 	Product Data: Include product description for bullet-resistant sheet including bullet-resistant ratings.

- Sustainable Design Submittals:

1. 	Regional Materials: Indicate cost of products harvested, extracted, recovered, or manufactured within 500 mile radius of Project site.

1.5 	WARRANTIES

A. 	Provide manufacturer’s 2 year warranty providing coverage against defects in materials and workmanship.

Action Bullet Resistant	10-2641	Bullet-Resistant Fiberglass Sheet

08/31/15

# PART 2 	PRODUCTS

2.1 	MANUFACTURERS

- Contract Documents are based on products by Action Bullet Resistant, 235 Union Blvd., West Islip NY 11795,800-962-8088, www.actionbullet.com.

- Substitutions: [Under provisions of Division 01.] [Not permitted.]

2.2 	MATERIALS

A. 	Bullet-Resistant Fiberglass Sheet:

  - Source: Opaque Fiberglass.

  - Description:

    - Manufactured from multiple layers of woven roving ballistic grade fiberglass cloth impregnated with thermoset polyester resin, compressed into flat rigid sheets.

    - Provide controlled internal delaminating to permit capture of penetrating projectile.

  - Ballistic Level: [1,] [2,] [3,] [4,] [5,] [6,] [7,] [8,] tested to UL 752.

  - Fire rating: 1 hour, tested to ASTM E119.

2.3 	ACCESSORIES

A. 	Adhesives and Fasteners: Type recommended by bullet-resistant sheet manufacturer for specific application.

# PART 3 	EXECUTION

3.1 	INSTALLATION

- Install in accordance with manufacturer’s instructions.

- Cut panels to fit at perimeter and around penetrations.

- Reinforce joints between sheets with minimum 4 inch wide backup layer of bullet-resistant sheet, centered on joint. Bullet-resistance of reinforced joint at least equal to ballistic level of panel.

- Fasten or adhere panels to supports in manner to maintain bullet-resistive rating at perimeter, junctures with other materials, and penetrations.

END OF SECTION